## Slide 1: Quantum Fluorescent Gold and Superparamagnetic Iron Oxide Nanoparticles for Biomedical Sensing
Regina Maria Chiechio, Antonino Scandurra, Stefano Boscarino, Cristiano Lo Pò, Riccardo Reitano, Paolo Musumeci, Maria Grazia Grimaldi, Maria Chiara Spadaro, Francesco Salutari, Salvatore Baglio, Salvatore Graziani, Annalinda Contino, Giuseppe Maccarrone, Thierry Guizouarn, Olivier Hernandez, Valerie Marchi, Ludovica Maugeri, Salvatore Petralia, Francesco Ruffino.
PE4 NQSTI
Spoke 7
Notes: “Good morning everyone, my name is Regina Maria Chiechio, I am a researcher at the University of Catania and part of Spoke 7 of the NQSTI project. In this talk, I will present our recent work on quantum fluorescent gold and superparamagnetic iron oxide nanoparticles for biomedical sensing.”

## Slide 2
SPOKE 7 Complete Quantum Systems
Spoke 7 is focused on the application-oriented development of complete quantum systems based on novel ideas developed in collaboration with spokes 1 and 2, as well as integrated devices and modules that have been simulated, designed and tested in spokes 3, 4, 5 and 6
A7.1 Imaging Systems
A7.2 Point Sensing Systems
A7.3 Communication & IoT Systems
A7.4 Simulation Systems
Activities
A7.2.1: Development of spectroscopy-based sensing system for biomedical and environmental inspection.
A7.2.2: Development of chemical sensing systems for biomedical applications
Quantum Nanostructures for environmental and biomedical sensing
1

## Slide 3
Luminescent Gold Nanoclusters (Au NCs)
Au NCs luminescence mechanism
Fe3O4 NPs for magnetic field sensing
Au NCs based sensor
Outline
2

## Slide 4
Gold Nanoclusters (Au NCs)
Au NCs
d~2nm
Luminescent
Photostable
High
Biocompatibility
Applications:
Bioimaging
Theragnostic
Drug delivery
Radiosensitizers
C3E6D Blue NCs
GSH Red NCs
GSH IR NCs
Biosensing
(Mussa F. et Al., Prog. Mater. Sci – 2024)
Blood concentration of Au NCs
(Zhang et Al., Scientific Reports – 2015)
3

## Slide 5
Au NCs: Quantum luminescence
(Shell)
LUMOs
HOMOs
(Ligand)
(Metal)
Diagram of energy levels of NCs.
(Kevin G. Stamplecoskie et al.- 2013)
(Core)
Red NCs
IR NCs
Blue NCs
(LT ≃ 1ns)
(LT ≃ 0.1 µs)
(LT ≃ 1 µs)
4

## Slide 6
Au NCs: Synthesis
HR-TEM
5nm
Crystalline
1 nm
Size ≃ 2,4 ± 0,5 nm
HAuCl4
GSH NCs
λex=420 nm
λem= 620 nm
GSH
GSH
Regina M. Chiechio et Al., The Journal of Physical Chemistry Letters - 2022
GSH
5

## Slide 7
GSH NCs Liquid Sensor
dsDNA
S
ssDNA-probe
S
ssDNA-target
6

## Slide 8
Kinetic study
Zetametry
-7
-20
-40
PL
R. Chiechio et Al., Applied Surface Science Advances - 2025
ssDNA-probe
S
ssDNA-target
7

## Slide 9
Target at different concentrations
PL
R. Chiechio et Al., Applied Surface Science Advances - 2025
LOD: 25 aM
Hill Model:
(Li, W et Al., Nanoscale Adv. – 2020)
8

## Slide 10
Compl | NON Compl
Kd = 0.04 ± 0.07 fM | Kd = 10 ± 15 fM
n = 0.15 | n = 0.26
Vmax: 30 % | Vmax: 17 %
LOG
Specificity Tests
Blood Test
R. Chiechio et Al., Applied Surface Science Advances - 2025
9

## Slide 11
Silanized ITO-PET
100 µm
Confocal microscope
Excitation wavelength (nm)
Emission wavelength (nm)
Solid
Liquid
Excitation wavelength (nm)
Emission wavelength (nm)
Photoluminescence MAP
Solid sensor prototype
10

## Slide 12
Chapter 11. Magnetic Nanoparticles for Application in Biomedical Sensing
Iron Oxide Nanoparticels (IONPs)
11

## Slide 13
Iron Oxide NPs synthesis
12
Iron target
NPs
Laser beam
GSH
Citrate
H2O
R. Chiechio et Al., Journal of Physics and Chemistry of Solids - Submitted

## Slide 14
IONPs: Morphological characterization
200 nm
GSH
200 nm
Citrato
d≃9 nm
200 nm
H2O
TEM
SEM
13
R. Chiechio et Al., Journal of Physics and Chemistry of Solids - Submitted

## Slide 15
STEM-EELS
Fe
O
Fe - O
H2O
HR-TEM Diffraction
5 nm
GSH
Fe3O4
5 nm
Citrate
Fe2O3
H2O
Fe3O4
Fe2O3
Fe3O4
RAMAN
14
IONPs: Compositional characterization
R. Chiechio et Al., Journal of Physics and Chemistry of Solids - Submitted
SQUID

## Slide 16: Solid Sensor: IONPs anchoring on substrate
Nylon
or cotton
Fe3O4 NPs
600 nm
H2O
600 nm
Citrate
200 µm
Cotton
100 µm
Nylon
15

## Slide 17
Optical, chemical and magnetic biosensing for biomedical and environmental applications
Silanized ITO-PET
Synthesis and characterization of quantum nanostructures
16
Conclusions

## Slide 18: Thanks

## Slide 19
Thank you for your attention!

## Slide 20
Khalid, A. et al. Lifetime Reduction and Enhanced Emission of Single Photon Color Centers in Nanodiamond via Surrounding Refractive Index Modification. Sci Rep 5, 11179 (2015).
Perspectives
Nanodiamonds: Quantum Biosensors
17
Su, J., et Al (2025), Fluorescent Nanodiamonds for Quantum Sensing in Biology. WIREs Nanomed Nanobiotechnol, 17: e70012.

## Slide 21
dsDNA
S
ssDNA-probe
S
ssDNA-target

## Slide 22
Target at different concentrations
LOD: 32 pM
Sensitivity: 14498 cps/nM
Kd=2.96 nM
n=0.466
Hill Model:
(Li, W et Al., Nanoscale Adv. – 2020)
PL
5
R. Chiechio et Al., Applied Surface Science Advances - 2025

## Slide 23
Higher probe concentration
LOD: 25 aM
Photoluminescence
6
R. Chiechio et Al., Applied Surface Science Advances - 2025

## Slide 24
STEM-EELS
Fe
O
Fe - O
H2O
HR-TEM Diffraction
5 nm
GSH
Fe3O4
5 nm
Citrate
Fe2O3
H2O
Fe3O4
Fe2O3
Fe3O4
RAMAN
14
IONPs: Compositional characterization
R. Chiechio et Al., Journal of Physics and Chemistry of Solids - Submitted
SQUID
300 K
5 K
SQUID

## Slide 25
GSH
Citrate
H2O
Iron target
NPs
Laser beam

## Slide 26
0
I
Excitation coil
Pick-up
coil
Ferromagnetic core
Fluxgate magnetometer
Salvatore Graziani
Salvo Baglio
Claudia Ferro
Piero D’Arrigo
Residence Times Difference
m
U(m)
m
U(m)
Notes: This sensor is an innovative device to detect quasi-static perturbations of the external magnetic field.
The sensor is composed of two sections: 1) a primary coil 900 turns, and 2) a secondary coil 900 turns.
The coils are wound around a flexible ferromagnetic core (having a diameter of about 100 μm.
A periodic voltage is applied to the excitation coil (Vin); hence, a periodic magnetic field He, parallel to the long axis of the core, is generated. Hx is the quasi-static “target” magnetic field, which represents (in this case) the iron compounds in the brain. The magnetometer works by exploiting the information measured through the pick-up coil (Vout signal).
The produced magnetic field is symmetric, while the external magnetic field create an asymmetry in the potential and then in the pick-up coil tension.
The voltage response is a “spike train,” the first derivative of the core magnetization. The distance between two spikes is not equal passing to a polarization to the other, since the target external field create an asymmetry. So the sensor measure the difference between this two time of magnetization (positive and negative) to quantify the external field.
By changing the magnetic property of the material, as a smaller coercive field and a higher permeability, it is possible to obtain a sensor more rapid e more sensible. And we wanted also to create a wereable sensor by increasing the core flexibility without breaking the magnetic domain. So we want to improve the functional and structural properties.
RTD = T+ − T −.
In the absence of an external magnetic field, the RTD = 0
B= Magnetic Field Density

## Slide 27
Plastic
or fabric
0
I
Excitation coil
Pick-up
coil
Ferromagnetic core
Flexible ferromagnetic core
Fe3O4 NPs
Fluxgate magnetometer
Salvatore Graziani
Salvo Baglio
Claudia Ferro
Piero D’Arrigo
Notes: This sensor is an innovative device to detect quasi-static perturbations of the external magnetic field.
The sensor is composed of two sections: 1) a primary coil 900 turns, and 2) a secondary coil 900 turns.
The coils are wound around a flexible ferromagnetic core (having a diameter of about 100 μm.
A periodic voltage is applied to the excitation coil (Vin); hence, a periodic magnetic field He, parallel to the long axis of the core, is generated. Hx is the quasi-static “target” magnetic field, which represents (in this case) the iron compounds in the brain. The magnetometer works by exploiting the information measured through the pick-up coil (Vout signal).
The produced magnetic field is symmetric, while the external magnetic field create an asymmetry in the potential and then in the pick-up coil tension.
The voltage response is a “spike train,” the first derivative of the core magnetization. The distance between two spikes is not equal passing to a polarization to the other, since the target external field create an asymmetry. So the sensor measure the difference between this two time of magnetization (positive and negative) to quantify the external field.
By changing the magnetic property of the material, as a smaller coercive field and a higher permeability, it is possible to obtain a sensor more rapid e more sensible. And we wanted also to create a wereable sensor by increasing the core flexibility without breaking the magnetic domain. So we want to improve the functional and structural properties.
RTD = T+ − T −.
In the absence of an external magnetic field, the RTD = 0
B= Magnetic Field Density

## Slide 28
Fluxgate Magnetometer Applications
C. Trigona et Al. in IEEE Transactions on Instrumentation and Measurement, vol. 67, no. 4, pp. 971-980, April 2018
Fettin detection inside brain for neurodegenerative deseases
Volcanic ash fallout estimation
B. Ando1 et Al. 2008 - IEEE International Instrumentation and Measurement Technology Conference
9

## Slide 29
Iron Oxide Nanoparticles
Iron target
NPs
Laser beam
GSH
Citrate
H2O
Excitation
Coil (Ie)
Pick-up
Coil (Vout)
Nylon
or cotton
Fe3O4 NPs

## Slide 30
STEM-EELS
200 nm
O
Fe
Fe - O
Citrate
C
Fe
O
Fe - O
H2O
O
Fe
C - N
N
C
Fe - O
GSH
a)
b)
c)
Compositional characterization

## Slide 31
Fe2O3
Fe3O4
Raman Shift cm-1
Compositional characterization
5 nm
GSH
5 nm
Citrate
H2O
(02-2)
(20-2)
(2-20)
[111] Fe3O4
(2-20)
[110] Fe3O4
(004)
(1-1-3)
(-11-3)
{-101-5}
{-1-12-2}
Fe2O3
HR-TEM Diffraction
RAMAN
XRD

## Slide 32
SQID measurements M(T)
500 Oe
SQID measurements M(H)
300 K
5 K
Magnetical characterization
Notes: Magnetical characterization (SQID)

## Slide 33
Spettroscopia dei Difetti Emettitori di Singoli Fotoni nel Diamante
Questo studio esplora le proprietà spettroscopiche dei centri di colore nel diamante che fungono da emettitori di singoli fotoni (SPE). Questi difetti atomici mostrano caratteristiche di antibunching, e quindi emissione di fotoni singoli.
Amanuel Michael Berhane, Spectroscopy of single photon emitting defects in Gallium Nitride and Diamond, 2018
(a) Struttura atomica del centro NV nella cella unitaria del diamante (b) Spettro di un centro NV che mostra il picco di fluorescenza del NV- a 637 nm.

## Slide 34
Diamante con centri NV: robustezza e lettura di spin
Stabilità ottima
Fotoluminescenza intensa e stabile a temperatura ambiente, anche in condizioni ambientali variabili
Proprietà di spin
Accesso ottico allo stato di spin, utile per magnetometria e termometria quantistica
Versatilità di formato
Disponibile come punte AFM, film sottili o nanoparticelle per diverse geometrie di sensing
Caratteristiche:
Limitazione principale: Richiede strumentazione e processi di fabbricazione altamente specializzati
Applicazione ottimale: Misurazioni locali ad alta sensibilità (campi magnetici, temperatura) con risoluzione nanometrica.
I centri NV (Nitrogen-Vacancy) nel diamante combinano proprietà ottiche e di spin che li rendono ideali per applicazioni di sensing quantistico.
Qureshi, S.A. et Al., «Recent Development of Fluorescent Nanodiamonds for Optical Biosensing and Disease Diagnosis». Biosensors 2022, 12, 1181

## Slide 35
Khalid, A., Chung, K., Rajasekharan, R. et al. Lifetime Reduction and Enhanced Emission of Single Photon Color Centers in Nanodiamond via Surrounding Refractive Index Modification. Sci Rep 5, 11179 (2015). https://doi.org/10.1038/srep11179

## Slide 36
Su, J., Kong, Z., Zeng, L., Kong, F., Xia, K., Shi, F. and Du, J. (2025), Fluorescent Nanodiamonds for Quantum Sensing in Biology. WIREs Nanomed Nanobiotechnol, 17: e70012.

## Slide 37
13
Qureshi, S.A. et Al., «Recent Development of Fluorescent Nanodiamonds for Optical Biosensing and Disease Diagnosis». Biosensors 2022, 12, 1181

## Slide 38
Khalid, A. et al. Lifetime Reduction and Enhanced Emission of Single Photon Color Centers in Nanodiamond via Surrounding Refractive Index Modification. Sci Rep 5, 11179 (2015).
Qureshi, S.A. et Al., «Recent Development of Fluorescent Nanodiamonds for Optical Biosensing and Disease Diagnosis». Biosensors 2022, 12, 1181
Perspectives
Nanodiamonds: Quantum Biosensors
17

## Slide 39
Takuya F. Segawa, Ryuji Igarashi,
Nanoscale quantum sensing with Nitrogen-Vacancy centers in nanodiamonds – A magnetic resonance perspective,
Progress in Nuclear Magnetic Resonance Spectroscopy,
Volumes 134–135,
2023,
Pages 20-38,
ISSN 0079-6565,